Data Table

Table 1 – The data table organizes all calculations and details for each separate composition trial. Flexural strength and flexural modulus are presented in their respective units (MPa and GPa). The table also includes physical dimensions and sample ID numbers.

| Sample ID | Composition | Average b (mm) | Average h (mm) | Flexural Strength (MPa) | Flexural Modulus (GPa) |
| --- | --- | --- | --- | --- | --- |
| 1 | Neat epoxy resin | 9.625 | 6.2 | 5.58 | 3.77 |
| 2 | Resin + X layers woven glass fiber (continuous) | 9.725 | 10.15 | 4.32 | 3.07 |
| 3 | Resin + X layers woven glass fiber (continuous) | 9.825 | 9.0 | 7.54 | 4.36 |
| 4 | Resin + chopped glass fiber | 9.925 | 9.3 | 3.35 | 3.78 |
| 5 | Resin + chopped glass fiber | 9.575 | 11.2 | 3.10 | 2.32 |

Figure 1 – The epoxy resin plot showcasing a max force of 530 N. The left graph displays the full raw data, while the right graph highlights the linear fit, including the corresponding equation for a selected set of linear points to characterize the slope.

Figure 2 - The continuous fiber composite plot (trial 2) shows a maximum force of 1123 N. The left plot displays raw tabulated data, while the right plot highlights the chosen linear region used to characterize the slope. Note the sharp increase in maximum force. Also note, that the discrepancies in the raw data may be due to user error, such as inconsistent application of force on the sample.

Figure 3 - The continuous fiber composite plot (trial 3) shows a maximum force of 1572 N, indicating another steady increase from the first trial of the composite material. The left plot displays the raw data, while the right plot highlights the linear region used to characterize the slope, with the slope equation shown on the plot. Notably, the raw data plot is much more consistent compared to the previous trial.

Figure 5 – The second trial of the chopped fiber plot shows a maximum force of 947 N, a significant increase from the first trial of the chopped fiber composition. The left plot displays the raw data, while the right plot highlights the linear region used to characterize the slope.

Figure 4 - The chopped fiber plot shows a maximum force of 761 N, significantly lower than the two continuous fiber trials. The left plot displays the raw data, while the right plot highlights the linear region, with the trendline shown in red to characterize the slope. Notably, the raw data curve is much smoother and less choppy compared to previous trials.